## Slide 1: Measuring Mechanical Properties of Thin Optical Coatings
Elaine Rhoades
Mentors: Dr. Zanolin and Dr. Gretarsson, Embry-Riddle
Collaborator: Dr. Abernathy, Caltech
April 4, 2014 Discovery Day

## Slide 2: Acoustics Setup
Image credits: Dr. Andri Gretarsson, ERAU
Notes: * Acoustics setup
Use a transducer to emit and sense reflections of a 0.4 GHz, 10 ns acoustic pulse from the surface of a sample.
Materials affect the reflected amplitude differently
Reflected amplitude contains information about the Young’s Modulus
* Thermocouple
Water absorption likely has a temperature dependence
Experimental setup has a thermocouple inserted between the piezo and spacers, which allows us to monitor the water’s temperature during data collection

## Slide 3: Acoustics Sample Data
Image credits: Justin Weber, ERAU

## Slide 4: Improvements to acoustics analysis
Automated the data windowing process
Introduced the use of a Tukey window to remove high frequency components
Introduced error propagation

## Slide 5: Improvements to acoustics analysis
Account for frequency-dependent distortions
  Water absorption
Investigate an attenuation effect with functional form
  g(f) is some function that depends on frequency
  d is water thickness
Use known materials to determine the values of g(f) that cause experimental values to match theoretical values
Apply analytically determined g(f) values to tantala
Physical interpretation of g(f) still unknown

## Slide 6: Frequency Dependent Distortion Estimation
Frequency (MHz) | Estimated g(f) Units of
330.6 | 
371.9 | 
413.2 | 
454.6 | 
495.9 | 
Frequency (MHz) | 
330.6 | 
371.9 | 
413.2 | 
454.6 | 
495.9 | 
Tantala fit values before correction
  E = 117.8 + 5.9 – 4.3 GPa
  σ = 0.319
Tantala fit values after correction
  E = 158.6 + 4.4 – 3.0 GPa
  σ = 0.233

## Slide 7: Acoustics Output

## Slide 8: Nanoindentation at Caltech
Image credits: Dr. Matt Abernathy, Caltech

## Slide 9: Nanoindentation Output
Image credit: Dr. Matt Abernathy, Caltech

## Slide 10: Comparison of Acoustics and Nanoindentation
Colored background is the acoustics chi-squared plot
Bold dashed line is the nanoindentation fit
Solid white lines are the errors in the nanoindentation fit

## Slide 11: Future Work
Take more data with acoustics setup
Continued collaboration with Matt Abernathy to finish nanoindentation analysis
Use techniques described to combine acoustics and nanoindentation to get results for a variety of samples

## Slide 13: Samples
Silica
Sapphire
Silicon cantilevers (borrowed from Glasgow group)
Silicon windows
Single-layer tantala coatings, base silica
Photo credit: Dr. Andri Gretarsson, ERAU

## Slide 14: Asymmetry of chi-squared plots
The first derivative has a zero at the minimum
The second derivative has some curvature
Taylor expansion of the fit function will give higher order corrections
Since the range we’re considering is larger than where the parabolic approximation is valid, see some non-linear effects from higher order derivatives